## PART 1: MULTI PANEL SYSTEM GENERAL

  - INTRODUCTION

Supply and fix Luxalon Multi-Panel System as manufactured by Hunter Douglas Architectural Products.

  - DESCRIPTION OF THE SYSTEM

The system will consist of box-shaped linear panels fixed to an adjustable suspension system which allows for individual panels to be removed by hand. System to feature open joins between the panels that can optionally be closed by clipping in join profiles. Panels of different widhts can be combined in one ceiling.

## PART 2: PRODUCT

_________m2 Luxalon® Multi-Panel Ceiling, featuring a 20 mm* open join and

consisting of:

*30BXD ceiling panels can be featured with a 30 mm open joint

  - PANELS

- 30B, size 30x15 mm, rollformed from 0.35 mm Aluminium strip

- 80B, size 80x15 mm, rollformed form 0.5 mm Aluminium strip

- 130B, size 130x15 mm, rollformed from 0.5 mm Aluminium strip

- 180B, size 180x15 mm, rollformed from 0.6 mm Aluminium strip

- 30BD, size 30x39 mm, rollformed from 0.5 mm Aluminium strip

- 30BXD, size 30x64 mm, rolformed from 0.5 mm Aluminium strip

- 80BXD, size 80x64 mm, rolformed from 0.6 mm Aluminium strip

- 130BXD, size 130x64 mm, rolformed from 0.6 mm Aluminium strip

JOIN PROFILES

- Recessed V-shaped join profile, width 20 mm, manufactured from 0.2 mm Alumnium

- Recessed U-shaped join profile, widht 20 mm, manufactured form 0.2 mm Aluminium

Panels to be manufactured from prepainted, stove enamelled aluminium, alloy, EN-AW-5050 or equivalent (according to EN 1396 and ECCA).

Join profiles to be manufactured from prepainted, stove enamelled aluminium, alloy EN-AW-6011.

Panels have square sides and are plain/perforated (except 30B), with/without  non-woven acoustic textile. Panels to have a length of _________mm (manufacturer availability 800-6000 mm and on request  > 6000 mm). Panels to be coupled in longitudinal direction by means of panel splices.

Join profiles to allow for easy clipping into the open joint, without the use of additional tools.

  - SUSPENSION

Rows of 0.5Fe/0.95 Alu rollformed carriers shall be installed at ________centre on centre by means of adjustabel suspensions at a distance of_______, center on centre. Carriers will be joined by means of carrier splices. Carriers provided with prongs to hold panels in a module whick is a muliple of 50 mm.

## PART 3: ADDITIONAL SPECIFICATIONS

3.1 PERIMETER PROFILES

- Clip-on U-profile 28.6x16x20 mm, made of 0.35 mm thick aluminium

- Wall L-profile 29.2x19.4 mm made of 0.5 mm thick aluminium

- Wall L-profile 45x18.5 mm made of 0.8 mm thick steel/aluminium

- Wall W-profile, 45x21x21`x18.5 mm, made of 0.8 mm steel/aluminium

3.2 PERFORATIONS

Manufacturer shall supply Luxalon® Multi-Panel panels with following perforation specifications:

- ( 1.0 mm, ( 2 mm with 23% open area: for 30BD and 80B panels

- ( 1.5 mm, ( 3 mm with 23% open area: for 30BXD and 80BXD and 130BXD panels

- (  2.0 mm, ( 5 mm with 16% open area: for 30BD, 80B, 130B and 180B panels

Perforated panels to have a nominal plain border along the longitudinal panel direction to assure a maximum flatness and product stability:

- 80B panel, (1 mm perforated to have a plain border of 5 mm

- 80B, 130B and 180B panel, ( 2 mm perforated to have a plain border of 4 mm

- 30BD panels are perforated into the sides of the panels over a height of 18.5 mm for ( 1 mm and a heigth of 19.5 mm for ( 2 mm.

- 30BXD, 80BXD and 130BXD perforated into the side of the panel over a height of 41 mm.

  - ACOUSTICS

Manufacturer shall supply acoustic non-woven tissue, thicknes 0.2 mm factory applied inside the panels. Alternatively the installler can place individually PE wrapped mineral wool pads.

  - COATING

Architect will make a colour selection from the standard Hunter Douglas colour range for Luxalon® Multi-Panel panels code no.____or a special colour will made to match.

The coating will consist of a tough and durable 2-layer polyester finish in nominal thickness of 20 microns, applied in a continuous coil-coating process ensuring uniform coating and absolute adhesion.

  - INSTALLATION

All materials shall be installed in strict compliance with all local codes, ordinances and manufacturers recommandations including specific additional requirements as may be called for in the specifications or shown on the drawings.