## PART 1. GENERAL

  - INTRODUCTION

Supply and fix type “System” semi-concealed Veneered Wood Tile Ceiling System as manufactured by Hunter Douglas Architectural.

  - DESCRIPTION OF THE SYSTEM

The system will consist of wood veneer tiles mounted into a  24 mm slotted tee bar system, kept in place with compressing springs to guarantee straight alignment.

## PART 2. PRODUCT

  - VENEERED WOOD TILES

________m2 type “System” semi-concealed Veneered Wood Tile Ceiling consisting of:

Square edged tiles which are 594x594 mm or 1194x594 mm (T24) module 600x600 or 1200x600. The tiles have a 16mm thick FR treated MDF (B,S1-d0) core veneered with 0.6mm thick slip/book matched veneer on the visible side. A 0.6mm compensating veneer is adhered to the reverse of the tile. The square edged tiles have a 4mm join.

  - SUSPENSION

Consists of pre-punched main tee sections installed in a grid by means of inserting cross tees which are designed to be used with the size of tile selected.

## PART 3: ADDITIONAL SPECIFICATIONS

  - EDGE COVER PROFILES

- L-profile 29 x 19 mm made of 1.5 mm thick aluminium in white colour

  - PERFORATIONS

Manufacturer shall supply tiles with perforation pattern type_______ with a nominal  plain border on all sides.

Perforations will have a ____ diameter hole in a regular/irregular pattern or ____ diameter slot with a ____mm length in a regular/irregular pattern resulting in a ____% open area.

  - ACOUSTICS

Manufacturer shall/shall not supply acoustic non woven textile, thickness 0.2mm  glued on reverse tile side.

  - VENEER TYPES

Tiles shall be supplied with crown/quarter cut veneer ___________ slip/book matched selected from the Hunter Douglas veneer selector or a special veneer.

Samples shall be supplied for approval prior to order.

The veneer is lacquered with a UV-polyacrylate varnish.

  - INSTALLATION

All materials shall be installed in strict compliance with all local codes, ordinances and manufacturers recommendations including specific additional requirements as may be called for in the specifications or shown on the drawings.

  - SUBSTITUTIONS

Ceiling installers wishing to submit proposals on systems other than the Hunter Douglas System Wood Tile Ceiling System shall, at least 10 days in advance of the bid date, submit to the architect complete descriptive information of the total system and performance data of tests made as a system. In addition include a list of similar installations of the proposed substitution. If approval is made an addendum will be issued enumerating such approved system as herein set forth.