## PART 1: GENERAL

  - INTRODUCTION

Supply and fix Luxalon® 70U Ceiling system as manufactured by Hunter Douglas Architectural Products.

  - DESCRIPTION OF THE SYSTEM

The system will consist of linear box shaped panels fixed to an adjustable suspension system which allows for individual panels to be removed by hand. System to feature open joints between the panels. The suspension system consists of a non Luxalon® levelled rigid suspension structure. To prevent contact corrosion by applying dissimilar metals, each fixing of the carriers to the sub-construction must be made through the Luxalon® washer set.

## PART 2: PRODUCT

_________m² Luxalon® Exterior 70U Ceiling, featuring a 30 mm joint and consisting of:

2.1 PANELS

Panels, 70 mm wide, 25 mm deep, to be roll formed from 0.8 mm thick stove enamelled aluminium strip, plain. Optionally acoustic pads can be laid on the panels in order to improve acoustical performance.

Aluminium panels to be manufactured from pre-painted, stove enamelled aluminium, corrosion resistant alloy EN-AW 3005 or equivalent (according to EN 1396 and ECCA).

Panels have a length of _________ mm (manufacturer availability 1000-6000 mm and on request 250-1000 mm and > 6000 mm). Panels to be connected in longitudinal direction by means of panel splices.

2.2 SUSPENSION

Rows of 0.95 Alu roll formed carriers shall be installed at _________ centre on centre by means of levelled suspensions of sufficient strength and rigidity to provide resistance to wind pressure/-suction, at a distance of _________, centre on centre. Carriers will be joined by means of carrier splices. Carriers provided with prongs to hold panels in a standard module of 100 mm.

Fixing clips made of enamelled aluminium, clipped on to the panel carrier between the panels in order to secure the panels.

## PART 3: ADDITIONAL SPECIFICATIONS

3.1 PERIMETER PROFILES

- Wall L-profile 29.2 x 19.4 mm made of 0.5 mm thick aluminium

- Wall L-profile 45 x 18.5 mm made of 0.8 mm thick aluminium

- Wall W-profile 45 x 21 x 21 x 18.5 mm made of 0.8 mm thick aluminium

3.2 COATING

Architect will make a colour selection from the standard Hunter Douglas colour range for Luxalon® 70U panels code no. _________ or a special colour will be made to match.

The coating will consist of a tough and durable Luxacote® finish in nominal thickness of 20 microns, applied in a continuous coil coating process ensuring a uniform coating. Luxacote® finish guarantees optimum adhesion and excellent resistance to weathering.

3.3 INSTALLATION

All materials shall be installed in strict compliance with all local codes, ordinances and manufacturers recommendations including specific additional requirements as may be called for in the specifications or shown on the drawings.