## PART 1: GENERAL

1.1 INTRODUCTION

Supply and fix Luxalon® Lay-On Tile Ceiling System as manufactured by Hunter Douglas Architectural Products.

1.2 DESCRIPTION OF THE SYSTEM

The system will consist of metal tiles laid into a 15 mm or 24 mm slotted tee bar system.

## PART 2: PRODUCT

2.1 TILES

________m2 Luxalon® Lay-in Tile Ceiling consisting of:

Square edged tiles which are 591x591 mm (module 600 x 600) or 616 x 616 mm (module 625 x 625) made of 0.5 mm thick steel. The square edged tiles are designed to lay on bottom flange of the tee bar.

2.2 SUSPENSION

Consists of pre-punched main tee sections installed in a grid by means of inserting cross tees which are designed to be used with the size of tile selected.

Maximum distance of rapid hangers fixing points on the main tee is 1200 mm. Main tees and cross tees will be finished standard baked white enamel finish. Matching colours to the tiles are available on request.

## PART 3: ADDITIONAL SPECIFICATIONS

3.1 EDGE COVER PROFILES

- L-profile 25  x  25 mm made of 1.5 mm thick steel aluminium

- W-profile 25 x 25 x 25 x  25 mm made of 1.5  thick aluminium

- F-profile, 25 x 25 mm, made of 1.5 thick aluminium

- Stepped F-Profile, 25 x 25 x 25 x 25 mm, made of 1.5 thick aluminium

3.2 PERFORATIONS

Manufacturer shall supply tiles with perforation pattern no.____ with a nominal 10 mm plain border on all sides.

Perforations will have a ________diameter hole resulting in a ____% open area. Other borders on request.

3.3 ACOUSTICS

Manufacturer shall supply acoustic non-woven textile thickness 0.2  mm glued into the tile or black faced PE wrapped mineral wool thickness___mm density____kg/m3 and of a size completely fill the tile.

3.4 COATING

Architect will make a colour selection from the standard Hunter Douglas colour range for Luxalon® Tiles RAL code no._______or a special colour will be made to match.

The coating will consist of a tough and durable polyester powder coating finish in minimal thickness of 60 microns, electro statically applied into electro-galvanised steel, phosphates and chemically treated according to high industrial standards (DIN 1541/ TAIM standards).

3.5 INSTALLATION

All materials shall be installed in strict compliance with all local codes, ordinances and manufacturers recommendations including specific additional requirements as may be called for in the specifications or shown on the drawings.

3.6 SUBSTITUTIONS

Ceiling installers wishing to submit proposals on systems other then the Luxalon® Tile Ceiling System shall, at least 10 days in advance of the bid date, submit to the architect complete descriptive information of the total system concept and performance data tests made as a system. In addition include a list of similar installations of the proposed substitution. If approval is made an addendum will be issued enumerating such approved system as herein set forth.